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Iron oxide black 725

Product data

 Iron Oxide Black 725 is an inert, non-toxic and high quality inorganic black pigment. Thanks to its stable chemical composition and structure, it is insoluble in water and dilute acids, resistant to acids, lime and alkalis, and absolutely resistant to weather and light.

Characteristics

Appearance: black pigment

Delivery form: powder

Chemical Grade: Synthetic Iron Oxide Fe3O4

Color index: pigment black 11 (77499)

CAS NO: 1317-61-9

Technical details

Fe3O4 content 92.0% min.

Tinting 95-105%

Color tone (△ E) 1.0 or less

The rest on a sieve (0,045 mm) no more than 0,4%

Humidity (after production) 1.0% max.

Oil absorption (g/100g) 15-25

pH value 4.0-8.0

Water soluble 0.5% max.

Applications

Iron oxide Black 725 has strong hiding power and features high tinting power, exceptional light fastness, strong UV absorption and fine dispersion, making it widely used as a colorant for cement products, paints and paints.

Main uses

 Coatings

 Construction

 Plastic

 Rubber

Packaging and storage

25kg/bag with pallet, wrapped and shrink bags 1000kg/1100kg with pallet.

Store it in its original packaging in a cool, dry and clean place away from direct sunlight. Open bags should be used immediately to avoid

moisture absorption.

The above information is based on our current experience and is offered for reference only. They do not release the user from testing and determining suitability for his own processes and applications. Tongchem makes no other warranties and makes no commitments, express or implied.
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