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Iron Oxide Jet Black 777
Product Data
Iron Oxide Jet Black 777 is an inert, non-toxic and high-quality inorganic black pigment. Due to the stable chemical composition and structure, it is insoluble in water and diluted acids, resistant to acid, lime and alkaline as well as absolutely weather and light stable.
Specifications
Appearance:                   Black pigment
Delivery Form:                       Powder
Chemical Class:     Synthetic iron oxide Fe3O4
Color Index:         Pigment Black 11 (77499)

CAS No．:                        1317-61-9
Techinlcal Data
	Fe3O4 content
	92.0% min

	Tinting strength
	95-105%

	Color Shade(△E)
	1.0 max

	Sieve Residue(0.045mm)
	0.4% max

	Moisture (After Production)
	1.0% max

	Oil absorption (g/100g)
	15-25

	pH value
	4.0-8.0

	Water soluble 
	0.5% max


Applications
Iron oxide Jet Black 777 has a strong covering power, and be characterized by its high tinting strength, outstanding light fastness, strong absorption of ultraviolet light and fine dispersing,  which make it widely used as colorant for cement  products, painting and inks..

Main uses
  Coatings
  Construction
  Plastic

  Rubber
Packaging & storage
25kg/bag with pallet, wrapped and shrank   1000kgs/1100kgs jumbo bags with pallet.
Keep it in cool, dry and clean conditions in its original packing, and avoiding direct sunshine. Opened sacks should be used promptly to avoid

the moisture absorption.
The above information are based on our current experience and offered merely for your reference. They do not release the consumer from making tests and determining the suitability for his own processes and applications. Tongchem makes no other warranties and assumes no liability, expressed or implied.
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