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Product Data          Iron Oxide Red 190
Iron Oxide Red 190 is an inert, non-toxic and high-quality inorganic pigment produced by mixed acid process. Due to the stable chemical composition and structure, it is insoluble in water and diluted acids, resistant to acid, lime and alkaline as well as absolutely weather and light stable.
Specifications
Appearance:                    Red pigment
Delivery Form:                       Powder
Chemical Class:   Synthetic iron oxide α-Fe2O3
Color Index:          Pigment red 101(77491)
CAS No．:                       1309-37-1
Techinlcal Data
	Fe2O3 content
	96% min

	Tinting strength
	95-105%

	Color Shade(△E)
	1.0 max

	Sieve Residue(0.045mm)
	0.3% max

	Moisture (After Production)
	1.0% max


	Oil absorption (g/100g)
	15-25

	pH value
	3.0-7.0

	Water soluble 
	0.5% max

	Lightfastness in full shade
	7-8

	Lightfastness tint shade (with titanium dioxide)
	7-8

	Weather resistance
	4-5

	Heat resistance
	200℃-  220℃

	resistance to Alkali
	3-4

	resistance to Acid
	4-5

	Resistance to solvent
	4-5


Applications
Iron Oxide Red 190 has better performance with its optimized color strength, superior dispersibility, chemical stability, and outstanding light fastness for painting and coatings. With the good opacity, high tinting strength, strong absorption of ultraviolet light, it is also used as colorant in other fields for construction industry.
Main uses
  Coatings

  Construction

  Plastic

  Rubber
Packaging & storage
25kg/bag with pallet, wrapped and shrank   1000kgs/1100kgs jumbo bags with pallet 
Keep it in cool, dry and clean conditions in its original packing, and avoiding direct sunshine. Opened sacks should be used promptly to avoid the moisture absorption.
The above information are based on our current experience and offered merely for your reference. They do not release the consumer from making tests and determining the suitability for his own processes and applications. 
Tongchem makes no other warranties and assumes no liability, expressed or implied.
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