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TECHNICAL DATA SHEET           Lemon Chrome Yellow  

Type Yellow Pigment

Delivery Form Powder

Chemical Class Lemon Yellow Pigment  2PbCrO4·PbSO4

Color Index Pigment yellow 34（77603）
CAS No．1344-37-2

Use Recommendation Coating/ Plastics/ Paper/ Print ect.

TECHNICAL DATA
Item                                       Standard 

Water-Soluble Content [%] max                1.0 
Sieve Residue（0.045mm）[%]  max          0.5 
PH Value                                    4.0-8.0
PbCrO4 [%]                    min           50.0

Moisture (After Production) [%]   max           3.0
Oil Absorption [g/100g]          max           25

Light fastness                                 5-6
STANDARD PACKAGING 25kg/bag
TRANSPORT AND STORAGE

Protect against weathering. Store in a dry place and avoid extreme fluctuations in

temperature. Special conditions for opened packaging: Close bags after use to prevent

the absorption of moisture and contamination.
SAFETY

The product is not classified as dangerous under the relevant EC directives and

corresponding national regulations valid in the individual EU member states. It is not

dangerous according to transport regulations. In countries outside the EU, compliance

with the respective national legislation concerning the classification, packaging,
REMARK

This information is given in good faith, without warranty. It is also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to verify the information currently provided and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General conditions of sale and delivery.

